- Purpose:

To define the procedure for determination of moisture content in solid biofuels by oven-drying method.

- Scope:

This procedure is applicable to the analysis of Biomass pellets, Briquettes, Agro-residues, Wood chips, Torrefied biomass and other solid biofuels.

- Definitions And Abbreviations:

  - Biomass Pellets

Densified solid biofuel produced by mechanically compressing milled biomass (e.g., sawdust, agro-residues) into cylindrical shapes, typically without chemical binders.

  - Briquettes

Solid biofuel blocks formed by compressing biomass under high pressure, generally larger than pellets and may contain natural binders inherent in biomass.

  - Agro-residues

Agricultural by-products remaining after harvesting or processing crops (e.g., rice husk, bagasse, groundnut shell, mustard stalk).

  - Wood Chips

Mechanically reduced wood pieces produced by chipping logs, branches, or wood waste, used as fuel without densification.

  - Torrefied Biomass

Biomass that has undergone mild thermal treatment (typically 200–300°C in absence of oxygen), resulting in improved fuel properties such as higher energy density and hydrophobicity.

  - Solid Biofuels

Solid fuels produced directly or indirectly from biomass, including but not limited to pellets, briquettes, chips, agricultural residues, and thermally treated biomass.

- Safety Precautions:

- Use appropriate personal protective equipment (PPE), such as heat-resistant gloves, when handling hot crucibles.

- Ensure proper ventilation when operating the muffle furnace to prevent exposure to fumes.

- Follow all laboratory safety protocols and guidelines.

- Apparatus:

- Hot Air Oven (Temperature range up to 110°C)

- Analytical Balance (0.001 g readability - minimum)

- Drying Dishes (Non-corrosive (silica, stainless steel or aluminium), with tight-fitting lids)

- Desiccator with active desiccant

- Tongs

- Stopwatch / Timer

- Reagents:

None required for this test method.

Desiccant (Silica gel / equivalent).

- Sample Handling and Preparation:

- Sample shall be prepared as per relevant sample preparation standard.

- Particle size: Typically, ≤1 mm (as applicable to product standard).

- Sample must be representative and properly mixed.

- Sample must be stored in an airtight container prior to testing.

- Procedure:

  - Preparation of Dish

- Clean and dry empty dish with lid.

- Place dish and lid in oven at 105 ± 2 °C for 30 minutes.

- Cool in desiccator to room temperature.

- Weigh and record mass (W₁).

  - Weighing of Sample

- Weigh approximately 1.0 g of prepared sample into dish.

- Spread sample evenly.

- Record combined weight (W₂).

  - Drying

- Remove lid and place dish with sample in oven.

- Dry at 105 ± 2 °C for a minimum of 2 hours (or as per sample type requirement).

- Cover dish with lid before removing from oven.

- Cool in desiccator for 20–30 minutes.

- Weigh and record final mass (W₃).

- Repeat drying (30-minute intervals) until constant mass is achieved.

- Calculation:

The total moisture % can be calculated by the below formula:

Moisture % = W3-W1W2-W1×100

Where:

W₁ = Mass of empty dish (g)

W₂ = Mass of dish + sample before drying (g)

W₃ = Mass of dish + sample after drying (g)

- Reference:

- Indian Standard IS 17655 (Part 2) : 2021, Solid Biofuels – Determination of Moisture Content – Oven Dry Method