# Purpose

To describe the methods for determination of volatile matter in coal samples.

# Scope

This procedure applies to the determination of volatile matter in coal samples analyzed at SMJ Lab. It covers all coal samples submitted for routine testing, quality control, and client reporting purposes.

# Normative Reference

## Indian Standard IS 436 (Part 1): 2024

Methods for Sampling of Coal and Coke.

## Indian Standard IS 1350 (Part 1): 2025

Methods of Test for Coal and Coke - Proximate Analysis.

# Definitions And Abbreviations

## Volatile Matter

The proportion of a coal sample that is released as gases during heating in an inert atmosphere.

# Safety Precautions

- Use appropriate personal protective equipment (PPE), such as heat-resistant gloves, when handling hot crucibles.

- Ensure proper ventilation when operating the muffle furnace to prevent exposure to fumes.

- Follow all laboratory safety protocols and guidelines.

# Apparatus

## Muffle furnace

Capable of reaching temperatures up to 900°C.

## Crucible and lid

Heat-resistant ceramic or porcelain

## Analytical balance

## Desiccator

## Tongs or crucible holder

# Reagents

None required for this test method.

# Sample Handling and Preparation

Pulverized coal sample is air-dried and passed through a 212-micron IS sieve.

# Procedure

- Weigh the crucible (W₁) using an analytical balance and record the weight.

- Place approximately 1 ±0.1 grams of the pulverized coal sample into the pre-weighed crucible.

- Cover the crucible with a lid and weigh the crucible and coal sample (W₂). Record the weight.

- Tap the crucible on a clean hard surface until the sample forms a layer of even thickness.

- Place the crucible with the coal sample in a muffle furnace preheated to 907 ±5°C.

- Heat the crucible at 907 ±5°C for 7 minutes in an atmosphere of nitrogen gas or another inert gas to prevent oxidation.

- After heating, remove the crucible from the furnace using tongs or a crucible holder and place it first on metal for 5 minutes and then in a desiccator for 10 minutes to cool.

- Once cooled, weigh the crucible and residue (W₃). Record the weight.

# Calculation

The volatile matter % can be calculated by the below formula:

| Volatile Matter % = | (W₂ – W₃) | x 100 |
| --- | --- | --- |
|  | (W₂ – W₁) |  |